## Slide 1
Packaging | 
Paper bags | á 25 kg
EVA bags | on demand
Big Bags | 600 - 900 kg
Bulk | on demand
Aktifit am
Paint & Varnish
1. Description
AKTIFIT AM is an activated SILFIT Z 91, produced by modifying the surface with an amino functional group. The by-products split off during the treatment reaction are largely removed during the production process which firmly attaches the functional group to the filler surface. This helps minimize undesirable side effects, as they are potentially encountered with in-situ mixing (direct addition of additive to the compound). During curing (hardening) of the coating, the amino groups of AKTIFIT AM react with appropriate functional groups of the binder or generate a strong interaction in the form of hydrogen bonds. .
Characteristics | 
Appearance | free-flowing powder
Color CIELAB scale: L* a* b* | 96.2 - 0.1 1.0
Residue > 40 µm | 10 mg/kg
Volatile matter at 105 °C | 0.2 %
Densitiy | 2.6 g/cm³
Particle size distribution D50 D97 | 2.3 µm 11.0 µm
Surface area BET | 9 m²/g
Oil absorption | 65 g/100 g
Electrical conductivity | 60 µS/cm
Equilibrium moisture content at 23 °C: 50 % relative humidity 80 % relative humidity 90 % relative humidity | 0.11 % 0.29 % 0.55 %
Shelf life
2 years if stored properly under dry conditions.

## Slide 2
Aktifit AM
Field of application: Paint & Varnish
2. Applications
In paint and varnish applications AKTIFIT AM can be used as functional filler either on its own or combined with extenders or matting agents. The best effect is achieved in binder systems which have functional groups with active hydrogen or which can react with. With inert, polar groups hydrogen bonds can be generated. In particular these include: epoxy resins polyurethane resins polyester resins alkyd resins acrylic resins phenolic and melamine resins all stoving enamel resins It stands out for its good wettability, excellent dispersion properties, which enable paint production potentially without grinding, very high brightness and color-neutrality. AKTIFIT AM enhances the opacity effect of pigments, thus it provides a replacement potential of titanium dioxide up to 20 %. In clear coats it achieves good transparency without yellow tint, a slight whitish glazing effect can result depending on formulation principle and loading. Beyond that it generates excellent mechanical properties with good scratch, abrasion and chemical resistance. Information on compliance with certain regulations/recommendations and other safety-related aspects: Product safety information
Fields of application
coil coatings can coatings stoving enamels powder coatings reactive industrial coatings anti-corrosion coatings primers and surfacers, also for the automotive industry adhesives and sealants Minimum film thickness: > 10 µm, less in special cases Dosage: up to 55 % depending on intended application likewise up to PVC 35

## Slide 3
Aktifit am
Field of application: Paint & Varnish
3. Benefits
The excellent properties of the base material SILFIT Z 91 are retained: low sieve residues low moisture content, low moisture absorption very high brightness very high color-neutrality outstanding dispersion behavior, even without grinding improved opacity (spacer effect), likewise potential for partial pigment replacement relatively low abrasivity quick drying weathering resistance scratch resistance abrasion resistance good transparency matting effect1 AKTIFIT AM also provides the following benefits compared with the base Silfit Z 91: improved wettability even using binders with medium polarity increased tensile and flexural strength as well as impact strength improved abrasion resistance and scratch resistance increased resistance to moisture, chemicals and weathering best grade for partial titanium dioxide replacement in polyester based can and coil coatings 1strongly dependent on formulation
4. Possible reaction in binder system
AKTIFIT AM + reactive group covalent bond filler to binder isocyanate methylol epoxy carboxy etc. AKTIFIT AM + polar group hydrogen bond filler to binder amide ester ether etc.

## Slide 4
Aktifit am
Field of application: Paint & Varnish
5. Application examples
Coil coating top coat
cost cutting potential by partial replacement of titanium dioxide up to 20 % slight reduction of gloss similar brightness L* and thus comparable hiding power color neutrality good weathering resistance slightly higher hardness improved scratch resistance Technical report: “Partial Replacement of Titanium Dioxide by Neuburg Siliceous Earth in a White Polyester-based Coil Coating Top Coat”
Can coating (polyester based)
cost cutting potential by partial replacement of titanium dioxide up to 20 %, for highly white and glossy about 10 %