## Slide 1
Packaging Options | 
Paper bag | 20 kg
EVA bag | 5 – 20 kg
Big bag | 550 – 900 kg
1. Material Description
AKTISIL PF 115/89 is an activated SILLITIN Z 89 in which the surface has been modified with a special amino-functional group. The byproducts released during the manufacture of AKTISIL grades are largely removed during the process. The coupling reaction fixes the functional group to the surface of the filler; undesirable side effects, such as those that occur during in-situ mixing (i.e., when the additive is added directly), are therefore virtually completely avoided. A special process technology used in the manufacture of AKTISIL PF 115/89 produces both partial hydrophobicity and reduced moisture absorption at high ambient humidity. During the cross-linking (curing) of the coating system, the amino groups of AKTISIL PF 115/89 react with suitable functional groups of the binder or form a strong interaction in the form of hydrogen bonds.
Characteristics | 
Appearance | Free-flowing powder
Color values according to CIELAB: L* a* b* | 96 0.2 3.8
Residue > 40 µm | 35 mg/kg
Volatile content at 105 °C | 0.3 %
Density | 2.6 g/cm³
Particle size distribution D50 D97 | 2.2 µm 10 µm
Oil absorption | 60 g/100 g
Water absorption according to Baumann | ≤ 0.1 ml/g
Equilibrium moisture content at 25°C 50% relative humidity 80% relative humidity 90% relative humidity | 0.16 % 0.27 % 0.45 %
Shelf life
2 years when stored in a dry, suitable location.
AKTISIL PF 115/89
Paint & Varnish

## Slide 2
AKTISIL PF 115/89
Application: Paint & Varnish
2. Applications
In the paint and varnish sector as well as in adhesives, AKTISIL PF 115/89 is used as a functional filler both on its own and in combination with extender fillers or matting agents. Optimal performance is achieved in binder systems that contain functional groups with active hydrogen or that can react with them. A strong interaction in the form of hydrogen bonds can also be formed with non-reactive, polar groups. These include, in particular: epoxy resins polyurethane resins acrylic resins alkyd resins polyester resins phenolic, melamine, and urea resins polysulfide systems all stoving paints/enamels in general adhesives, including those based on silane-terminated polymers (SMP, STP-E, STP-U) with increased strength Applications are wherever optimal wettability and very low sedimentation tendency are just as important as outstanding mechanical properties and high chemical and corrosion resistance. In solvent-free polar systems, AKTISIL PF 115/89 often increases viscosity at low shear rates. In aqueous anti-corrosion primers and DTM coatings, it often reduces blistering in the condensation water test and achieves good wet adhesion with minimal under-cutting at the scratch in the salt spray test. This potentially allows for a reduction in, or even complete replacement of, anti-corrosion pigments. AKTISIL PF 115/89 exhibits high brightness as well as color neutrality and is therefore also suitable for use in light-colored and color-sensitive applications. In adhesives, particularly those based on silane-terminated polymers, it achieves high strengths.
Fields of application
high-quality, reactive industrial coatings STP-based adhesives, reactive adhesives sealants and potting compounds baking enamels, including powder coatings corrosion protection coatings, including water-based and DTM acrylate, epoxy, including for clear coats high-solid fillers and primers, topcoats Minimum film thickness: > 10 µm, lower in special cases Dosage: up to 55% depending on the application.

## Slide 3
AKTISIL PF 115/89
Application: Paint & Varnish
3. Advantages
The excellent properties of the SILLITIN Z 89 base are retained: high brightness, high color neutrality excellent dispersibility good pigment distribution (spacer effect) low abrasivity very low tendency to settle soft sediment good edge-covering fast drying weather resistance breathability scratch resistance high abrasion resistance good transparency slight matting effect Compared to the base SILLITIN Z 89, AKTISIL PF 115/89 offers the following additional advantages: lower moisture content increased yield strength in polar systems with high solids content or 100% solids increased tensile and flexural strength as well as impact resistance improved abrasion resistance and scratch resistance increased chemical and moisture resistance improved corrosion protection increased gloss
4. Possible reactions in the binder system
AKTISIL PF 115/89 + reactive group covalent bond filler to binder isocyanate methylol epoxy carboxy etc. AKTISIL PF 115/89 + polar group hydrogen bond filler to binder amide ester ether etc.